Acoustical Diffuser Panel Specification for FRP Barrel Diffusers

SECTION 09840 – ACOUSTICAL DIFFUSER PANELS

PART 1 – GENERAL

1.1	SUMMARY

- This section includes the following:

- Acoustical Diffuser Panel

  - SUBMITTALS

- Shop Drawings: Show fabrication and installation details for acoustical diffuser panels, including plans, elevations, sections, details and attachment to other work.

- Submittals:  Furnish 8” x 8” samples, showing manufacturer’s full range of colors, texture and patterns available for each type of acoustical product specified.

- Product Test Report: From a qualified testing agency indicating diffuser panels comply with requirements.

- Qualification Data: For firms specified in “Quality Assurance” Article to demonstrate their capabilities and experience.

- Product Certificates: Signed by manufacturer certifying that the products furnished comply with requirements.

  - QUALITY ASSURANCE

- Manufacturer Qualification: Manufacturer shall have a minimum of 5 years experience in production of specified products and shall furnish supporting documentation showing completed jobs of approximately the same size and scope.

- Fire Test Reports: Provide acoustical diffuser panels with the following surface- burning characteristics as per ASTM E 84.

- Flame Spread: 25 or less

- Smoke Developed: 450 or less

- Acoustical Test Report: Provide acoustical test report from a qualified testing agency indicating acoustical wall panels meets specified NRC per ASTM C-423.

  - DELIVERY, STORAGE, AND HANDLING

- Protect Acoustical Diffuser Panels from excessive moisture when shipping, storing, and handling.  Deliver in unopened skids and store in a dry place with adequate air circulation.  Do not deliver material until all wet-work has been completed.

PART 2 – PRODUCTS

  - DIFFUSER PANELS, GENERAL

- Acoustical Diffuser Panels shall be (0.125”) thick fiber reinforced plastic. Lemon peel texture, white gel-coat finish or wrapped with panel manufacturers standard full line of fabric. (or custom fabric)

- Products

- Model Sound Quality FRP Barrel Diffuser

Sound Seal

Agawam, MA.  USA

Ph. (800) 569-1294

Fax (413) 789-4444

- Facing Material:

a. White lemon peel gel-coat

b.Guilford of Maine FR 701 – Style 2100 – 100% polyester                                           (or other)

- Panel Thickness: nominal (.125) thick

- Noise Reduction Coefficient:  NRC 0.15 or 0.05

- Panel Size: 2’ x 2’, 2’ x 4’, 3’ x 3’, 3’ x 4’, 4’ x 4’, (nominal), custom

  - CONSTRUCTION

- The acoustical diffuser panel product shall be supplied in sizes indicated.  All edges will be fully wrapped where applicable, with mounting as indicated.

  - MOUNTING

A.	Back-Mounting Accessories: Manufacturers standard accessories for securely mounting panels, of type and size indicated and complying with the following requirements:

- Two Part Mechanical Clip: One part mechanically attached to wall substrate, one part mechanically attached to the back of diffuser panel, with a leveling base to support brackets where indicated.

- Integral ceiling grid lay-in flange

2.4	ACOUSTICAL PERFORMANCE

Sound Absorption: Per ASTM C – 423

Sound Absorption Coefficient per Octave Band Center Frequency (Hz) Gel-coat finish

125	250	500	1000	2000	4000		NRC

.19	 .15	.07	.04	  .03	  .05		  .05

(Hz) Fabric finish

125      250      500      1000    2000    4000                NRC

.14       .21      .10       .09         .11       .19                   .15

2.5	FLAMMABILITY RATING

- All components shall have a Class A Flammability rating per ASTM E- 84:  Surface Burning Characteristics of Building Materials, with a Flame Spread of 25 or less and Smoke Developed of 450 or less

PART 3 – EXECUTION

  - INSTALLATION

- Install Acoustical Wall panels in locations indicated, top edges level and in alignment with other panels.   Comply with manufacturers written instructions for installation of panels using type of mounting accessories indicated or, if not indicated, as recommended by manufacturer.

  - CLEANING

- After completion of installation of panels, remove dust and other foreign material according to manufacturers written instructions.

- Remove surplus material, rubbish, and debris resulting from panel installation, on completion of the work, and leave areas of installation in a neat and clean condition.